Integrated Nano biocatalytic system for Shrimp shell Chitin Depolymerization

Shrihari G1, Sandra George1, Ben Johnson1, Priyadharshini Bharathi1 Vaidyanathan Vinoth Kumar1*

1Integrated Bioprocessing Laboratory, Department of Biotechnology, School of Bioengineering, Faculty of Engineering and Technology, SRM Institute of Science and Technology (SRM IST), Kattankulathur – 603203, Chengalpattu District, Tamil Nadu, India.

*Address for Correspondence: vinothkv@srmist.edu.in

Abstract

Shrimp waste constitutes a significant portion of global seafood byproducts, with over 6 million tons generated annually, posing serious environmental challenges. This study presents an integrated Nano biocatalytic system for efficient shrimp chitin saccharification and agro-waste valorization. Chitinase, a hydrolytic enzyme was produced using Bacillus thuriengiensis at 21 U/mL under optimized conditions (pH 6.5, 37°C), achieving 65% saccharification efficiency of shrimp chitin within 72 hours. Concurrently, sugarcane molasses, an agro-industrial byproduct, was utilized for the biosynthesis of sophorolipids by Starmerella bombicola, yielding 9.6 g/L. To enhance their functional properties, sophorolipids were conjugated with silver nanoparticles (AgNPs) using 1 mM AgNO₃, resulting in sophorolipid-AgNPs, characterized  by negatively charged (-35 mV) nanoparticles with a mean size of  <100 nm. The conjugates exhibited potent antimicrobial activity, with minimum inhibitory concentrations (MICs) of 25  µg/mL against Gram-positive bacteria and 50 µg/m against Gram-negative bacteria. Integrating sophorolipid-AgNPs with chitinase, a novel Nano biocatalytic system was developed, demonstrating 1.5-fold enhanced hydrolytic efficiency compared to free chitinase. This research highlights a sustainable approach to shrimp and agro-waste valorization, integrating advanced nanotechnology and biocatalysis. The developed system addresses global waste management issues while producing high-value bioproducts with broad applications in antimicrobial treatments and industrial biotechnology. Further studies are recommended to optimize scalability and explore broader commercial applications.

KEYWORDS: Bacillus thuringiensis (Bt), Shrimp, Chitin, Sophorolipids, Sophorolipids AgNP, Nano biocatalytic system.