Indigenously Developed Tunable Layered Dressings for the Treatment of

Infected Leg Ulcers

Arya Lakshmi.V.V1, Riju Menon2 and R. Jayakumar1*

1Polymeric Biomaterials Lab, School of Nanosciences and Molecular Medicine,

Amrita Vishwa Vidyapeetham, Kochi-682041, India

2Department of Surgery, Amrita Institute of Medical Sciences and Research Centre, Amrita Vishwa Vidyapeetham, Kochi 682041, India

*Corresponding author. Email: rjayakumar@aims.amrita.edu

Abstract

Chronic leg ulcer is a damage in the skin below the knee level that persists for more than a month where the usual course of healing is disturbed at different points across the phases of hemostasis, inflammation, proliferation, and remodeling. Chronic ulceration of the lower limb is a relatively common condition among older adults, and they can be caused by various underlying conditions, including venous insufficiency, arterial insufficiency and diabetes. They are often painful, recurring, and can significantly impair a person's quality of life and are manifested by prolonged inflammation, defective re-epithelialization and remodeling. The delayed healing process is caused due to overexpression of matrix metalloproteinase (MMPs) and is augmented by bacterial infection. To alleviate chronicity and enhance the wound healing process, it is imperative to reduce the overexpression of MMPs and lower the bacterial infection. Thus, we propose to develop a layered tunable dressing for treating infected leg ulcers. The bottom layer is composed of chitosan-alginate layer with doxycycline incorporation, serving as an antibacterial layer along with MMP2 & MMP9 inhibition. The top layer is composed of chitosan incorporated with potassium salt of sucrose octasulfate (SOS) and this layer promotes angiogenesis, thereby enhancing the wound healing process. The prepared layered dressings were characterized using SEM and FTIR. Porosity, swelling, and degradation percentage were studied and results showed high porosity, which facilitates exudate absorption, air circulation, and promote cell infiltration during healing. The swelling behavior ensures effective absorption and maintains a moist environment for optimal wound healing. The degradation profile of the layered dressing allows the bottom layer to degrade, releasing doxycycline to eliminate infection and inhibit MMP production. The inhibition of the proteolytic activity of MMPs was evaluated using gelatin zymography. The cumulative drug release percentage of doxycycline from the Cs-Alg-Doxy layer was measured, showing a sustained release profile that supports infection control and promotes wound healing. The antibacterial activity of the doxycycline incorporated bottom layer was studied and showed an antibacterial activity against Staphylococcus aureus and Escherichia coli. Additionally, anti-biofilm inhibition and membrane-disruption studies showed that the bottom layer of the layered dressing could inhibit biofilm formation and disrupt bacterial membranes. In vitro cell migration and cytocompatibility were assessed using the developed layered dressing and showed promising results in promoting cell migration and maintaining high cell viability, indicating its suitability for wound healing. Thus, the proposed layered dressing can act as an efficient wound dressing material to treat leg ulcers which has a higher potential to be clinically translatable with antibacterial activity, MMP2 & MMP9 inhibition and angiogenic properties.