In-situ synthesis of osteogenic & angiogenic chitosan-demineralised bone matrix-whitlockite composite bone filler

Sona Sunil, Arthi Chandramouli, R. Jayakumar

Polymeric Biomaterials Lab, School of Nanosciences and Molecular Medicine, Amrita Vishwa Vidyapeetham Kochi- 682041, India

*sona29sunil@gmail.com, rjayakumar@aims.amrita.aims.edu

Abstract

The rising demand for efficient and effective substitutes for bone tissue engineering has led to the development of novel biomaterials that are capable of regenerating and revascularizing bony defects. Currently, bioceramic-polymer composites such as chitosan-hydroxyapatite, collagen-hydroxyapatite etc are acquiring much attention in the field of bone tissue engineering. The recent biomaterials evolved to date lack the ability to mimic the natural composition of the bone. To address this constraint, we developed a chitosan-demineralised bone matrix-whitlockite (CS-DBM-WH) composite filler via an in-situ method. Chitosan (CS) is a biocompatible, biodegradable, antimicrobial and non-toxic biopolymer, which mimics the aminoglycosides in the extracellular matrix, thereby aiding in the process of regeneration. The presence of demineralised bone matrix (DBM) in the composite resembles the organic part of the bone containing collagen and other growth factors which promotes osteogenesis, whereas whitlockite (WH) being a bioceramic, imparts osteoconductive and osteoinductive properties, thereby simulating the inorganic part of the bone. The prepared CS-DBM-WH composite bone filler was characterized using FE-SEM, EDAX, XRD, FTIR and TGA analysis. FE-SEM images of CS-DBM-WH composite bone filler showed an average particle size of 270nm and EDAX analysis showed the elemental composition and confirmed the presence of whitlockite elements such as Ca, Mg and P. XRD and FTIR analysis exhibited the respective peaks of CS, DBM and WH in the prepared composite bone filler. The thermal stability of CS-DBM-WH composite bone filler was verified using TGA analysis. In vitro biocompatibility of the synthesised composite filler was studied using rat mesenchymal stem cells (rMSCs) and showed the biocompatible nature of the composite. This developed composite bone filler will be a promising candidate for regeneration of bone defects.